|  | ZHENGZHOU STEELL METAL CO.,LTD |
| --- | --- |
|  | Tel:0086 371 86080791 Fax:0086 371 67221140 E-mail:steellmetal@126.com |

CARBON PRODUCTS DATASHEET

- LOW NITROGEN GRAPHITE(GPC) – Fine Carbon additive and Inoculant

| LNG-100 | Chemical composition% |  |  |  |  |  |  |  | Minor element |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | F.C min |  | Ash max | V.M max |  |  | S max | Moisture max | N max | H max |
|  | 99.5 |  | 0.3 | 0.2 |  |  | 0.03 | 0.5 | 100ppm | 120ppm |
| Bulk density |  | approx 1.0g/cm3 |  |  | 1000Kg bags or on pallet approx 20MT,18MT/20FCL |  |  |  |  |  |
| Packing : 1000Kg bags, 25Kg paper bags , 1000Kg on pallet, or as users detail requirements. |  |  |  |  |  |  |  |  |  |  |
| Supply quantity:200-300MT/month; |  |  |  |  |  | Conventional grain size:1-5mm 90%min |  |  |  |  |

- Slag Foaming Carbons (Synthetic Graphite) for EAF steel making

| SGF-75 | Chemical composition% |  |  |  |  |  |  |  |  |  |  |  |  |  | Minor element |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | F.C |  |  | Ash approx |  | V.M |  |  |  | S approx |  |  | Moisture max |  | N max | H max |
|  | 75-80 |  |  | 20 |  | 1-3 |  |  |  | 0.3 |  |  | 0.5 |  | -- | -- |
| Bulk density |  | approx 1.3g/cm3 |  |  |  |  | 1000Kg bags or on pallet ; approx 20MT/20FCL |  |  |  |  |  |  |  |  |  |
| Packing : 1000Kg bags, 25Kg paper bags , 1000Kg on pallet, or as users detail requirements. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Supply quantity:180-200MT/month; |  |  |  |  |  |  |  |  | Conventional grain size:0.1-3mm 90%min |  |  |  |  |  |  |  |
| Ash composition % |  |  | Al2O3 |  | SiO2 |  |  | Fe2O3 |  |  | CaO | MgO |  | TiO2 |  |  |
|  |  |  | 45-47 |  | 7-9 |  |  | 3-5 |  |  | 3-5 | 1-3 |  | 0.2-1.0 |  |  |

- Black Silicon Carbide ( Metallurgy grade)

| BSIC-90 | Chemical composition% |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SiC |  | C-FREE | SiO2 |  | S max |  | Moisture max | Al2O3 max | Fe2O3 max |
|  | 88-92 |  | 3-6 | 3-6 |  | 0.5 |  | 0.5 | 0.4 | 0.5 |
| Bulk density |  | approx 1.9g/cm3 |  |  | 1000Kg bags or on pallet ; approx 20MT/20FCL |  |  |  |  |  |
| Packing : 1000Kg bags, 25Kg paper bags , 1000Kg on pallet, or as users detail requirements. |  |  |  |  |  |  |  |  |  |  |
| Supply quantity:600MT/month; |  |  |  |  |  |  | Conventional grain size:1-10mm 90%min |  |  |  |

- Silicon Carbide and Aluminum Oxide Production Complex(Refractory grade)

| ASIC | Chemical composition% |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SiC |  | Al2O3 |  |  | SiO2 | Fe2O3 | Carbon |
| SiCAL-75 | 20 approx |  | 50-75 |  |  | 3-9 | 0.5-2 | consultation |
| ALSIC-75 | 50-75 |  | 20 approx |  |  | 3-9 | 0.5-2 | consultation |
| Bulk density |  | 1.7- 1.9g/cm3 |  |  | 1000Kg bags or on pallet ; approx 20MT/20FCL |  |  |  |
| Packing : 1000Kg bags, 25Kg paper bags , 1000Kg on pallet, or as users detail requirements. |  |  |  |  |  |  |  |  |
| Supply quantity:3000MT/month; |  |  |  | Conventional grain size:8-5mm,5-3mm,3-1mm,20-325mesh etc. |  |  |  |  |

Regarding our company contents and other products ,please glance over:

www.steellmetal.com  ,  www.resteellmetal.com