|  | ZHENGZHOU STEELL METAL CO.,LTD |
| --- | --- |
|  | Tel:0086 371 86080791 Fax:0086 371 67221140 E-mail:steellmetal@126.com |

MINERALS PRODUCTS DATASHEET

- Slag Former for steel making in EAF , BOF ,LAF ,LADLE

| Al2O3-TFe-MAl Size:5-30mm 90% Packing:1000Kg bags |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Chemical Composition (%) |  |  |  |  |  |  |  |
| Al2O3min | SiO2 max | T-Fe max | M-Al | S max | P max | M-Si | C |
| 65 | 12 | 12 | 5 | 0.1 | 0.1 | 5.6 | consultation |
| 60 | 13 | 13 | 2 | 0.1 | 0.1 | 5 | consultation |
| 55 | 15 | 15 | 1 | 0.1 | 0.1 | 3 | consultation |
| Supply quantity:1000MT/month |  |  |  | Bulk density: approx 2.1g/cm3 |  |  |  |

2. Ladle filler sand

| Shape: Semi-round , Round; Size: 0.1-1mm,0.5-2mm,0.2-3mm,0.15-2mm; More than : 98% |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Chemical Composition (%) |  |  |  |  |  |  |
| Cr2O3min | SiO2 | Fe2O3 max | Al2O3 | MgO | Moisture max | C |
| 35 | 15-20 | 25 | 5-15 | 5-8 | 0.5 | 1.0 |
| 30 | 16-25 | 25 | 5-15 | 5-10 | 0.5 | 1.0 |
| 25 | 15-20 | 20 | 5-12 | 3-8 | 0.5 | 1.0 |
| Supply quantity:1000MT/month |  |  |  | Bulk density: approx 2.3g/cm3 |  |  |
| Refractories:1800℃ min |  |  |  | Coating Status: Coated Carbon |  |  |

3. Foundry Sand Additive-Spherical Ceramic Carbon Sand (SCS)

| Chemical Composition (%) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al2O3 | SiO2 |  | C | Fe2O3 | Fe3O4 | MgO | TiO2 | CaO |
| 70-75 | 7-12 |  | 3-9 | 1.2 | 1.3 | 0.7 | 0.3 | 0.2 |
| Shape: ball |  | Bulk Density:1.80-1.85g/cm3 |  |  |  | Refractoriness: 1850℃ |  |  |
| Size:40-270mesh 100%, AFS 50-AFS170 |  |  |  |  |  | Application : high quality sand castings |  |  |

4. Coil Grout (Red Mud)

| Application : inside face of core less induction furnace coils. |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Chemical Composition (%) |  |  |  |  |  |  |  |  |
| Al2O3min | SiO2 max | Fe2O3 max |  | CaO | TiO2 | Compressive Strength(Mpa) |  |  |
| 82 | 5.5 | 1.4 |  | 5.1 | 1.8 | 39（110℃/24h） |  |  |
| 86 | 5.0 | 1.4 |  | 5.0 | 1.6 | 39（110℃/24h） |  |  |
| Water Addition per 100Kg |  |  | 10-14Kg or liter |  | Initial Setting |  | 1.5h | Final : 4h |
| Supply quantity:120MT/month |  |  |  |  | Bulk density: approx 2.75g/cm3 |  |  |  |
| Refractories:1750℃ min(82 Al2O3) |  |  |  |  | Refractories:1800℃ min(86 Al2O3) |  |  |  |

Regarding our company contents and other products ,please glance over:

www.steellmetal.com  ,  www.resteellmetal.com