|  | ZHENGZHOU STEELL METAL CO.,LTD |
| --- | --- |
|  | Tel:0086 371 86080791 Fax:0086 371 67221140 E-mail:steellmetal@126.com |

CERAMICS PRODUCTS DATASHEET

- HIGH ALUMINA REFRACTORY FOR STEEL WORKS AND FOUNDRIES

| Product | Maximum Service Temperature | Bonding |  | Chemical Analysis (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Ramming mixes |  |  |  | Al2O3 | Si2O3 | Fe2O3 |
| ALURAM 75 | 1750°C /3180°F | Chemical |  | 75.0 | 20.0 | 2.0 |
| ALURAM 85 | 1750°C /3180°F | Ceramic |  | 82.7 | 12.8 | 1.5 |
| Mortar | Maximum Service Temperature |  | Bond Type |  | Al2O3 | Fe2O3 |
| MMOR-75 | 1810°C /3290°F |  | Air setting |  | 74.0 | 1.3 |
| CMMOR-85 | 1860°C /3380°F |  | Air setting |  | 81.0 | 0.7 |
| CMMOR-90 | 1860°C /3380°F |  | Air setting |  | 88.0 | 0.1 |
| Paint(Coating) | Maximum Service Temperature |  | Bonding | Al2O3 | SiC | C |
| P70 | 1860°C /3380°F |  | Chemical | 68 | 24 | 8 |
| P60 | 1860°C /3380°F |  | Ceramic | 65 | 29 | 6 |

- REFRACTORIES FOR THERMAL SPACE APPLICATIONS

| Product | Maximum Service Temperature |  |  | Color |  | Characteristics |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ceramic Microspheres |  |  |  | White Silver gray Black |  | Bulk Density |  |  | Diameter |
| CM-85 | 1860°C /3380°F |  |  |  |  | 1.70-1.95g/cm3 |  |  | 80-96μm |
| CM-80 | 1860°C /3380°F |  |  |  |  | 1.70-1.95g/cm3 |  |  | 45-75μm |
| Corundum Mullite Powder | 1860°C /3380°F |  |  | Color |  | Al2O3 | SiO2 |  | Fe2O3 |
| Bulk Density:2.1-2.3g/cm3 | Size:140-325mesh |  |  | Brown |  | 90% | 9.5% |  | 0.5% |
| Silicon Carbide Ceramic Powder |  | Color: Black ;SiC:95%min |  |  | Size:-100mesh,-200mesh |  |  |  |  |
| Ceramic Matrix Composites | Maximum ServiceTemperature |  |  |  | Color |  |  | Bulk Density | Fiber volume% |
| FCMC30 | 1750°C /3180°F |  |  |  | Silver gray Black |  |  | 1.5-1.75g/cm3 | 20-40 |
| FCMC50 | 1750°C /3180°F |  |  |  |  |  |  | 1.0-1.65g/cm3 | 40-60 |
| Producible Diameter 30-150μm |  |  | ILS(MPa) 55-70 |  | Flexural Strength(MPa) 700-800 |  |  |  |  |

Regarding our company contents and other products ,please glance over:

www.steellmetal.com  ,  www.resteellmetal.com